## Slide 1: SuperKEKB Review / Electron gun and transport
Mitsuhiro Yoshida
2015.02.24

## Slide 2
SuperKEKB upgrade for low emittance electron beam
 | KEKB obtained (e+ / e-) | SuperKEKB required (e+ / e-)
Beam energy | 3.5 GeV / 8.0 GeV | 4.0 GeV / 7.0 GeV
Bunch charge | e-  e+ / e- 10  1.0 nC / 1.0 nC | e-  e+ / e- 10  4.0 nC / 5.0 nC
Beam emittance (ge)[1s] | 2100 mm / 300 mm | 6 mm / 20 mm
High charge low emittance is required for SuperKEKB.
5 nC 10 mm-mrad electron beam generated by RF gun.
+ 10mm-mrad emittance preservation is required.
Preliminary test using DAW RF-Gun with Nd laser system
due to earthquake
Quasi –travelling side couple RF-Gun with Yb laser system
A
B
1
C
2
3
4
5
J-ARC
30ps
10ps

## Slide 3: RF-Gun for 5 nC
Space charge is dominant.
  Longer pulse length : 20 - 30 ps
Stable operation is required.
  Lower electric field : < 100MV/m
Focusing field must be required.
  Solenoid focus causes the emittance growth.
  Electric field focus preserve the emittance.
Total
Space charge
RF
Epaxial coupled cavity : BNL
Annular coupled cavity : Disk and washer / Side couple

## Slide 4: S-band RF-Gun development strategy for SuperKEKB
Cavity : Strong electric field focusing structure
  Disk And Washer (DAW) => 3-2
  Quasi Traveling Wave Side Couple => A-1
  => Reduce beam divergence and projected emittance dilution
Cathode : Long term stable cathode
  Middle QE (QE=10-4～10-3 @266nm) and long lifetime
  Solid material (no thin film) => Metal composite cathode
  => Started from LaB6 (short life time) => Ir5Ce has very long life time and QE>10-4 @266nm
Laser : Stable laser with temporal manipulation
  LD pumped laser medium
    Nd doped solid laser => 3-2
    Yb doped fiber and solid hybrid laser => A-1
  Temporal manipulation => Yb doped => Minimum energy spread

## Slide 5
Field
Focussing field
Accelerating field
Focussing field
Field
Given force
Given force
Focussing field
Focussing
field
=> Weak focus
=> Strong focus
Pill-box cavity
Annular coupled cavity with nose
Accelerating field
Accelerating field
Beam
Beam
Accelerating field
Accelerating field
Accelerating field

## Slide 6
Concentrated field has focusing effect
This structure has long drift space
Closed gap makes focus field
Side coupled cavity is one candidate (or DAW / ACS / CDS …)
This structure has focusing field.
Long drift space is problem.

## Slide 7
Normal side couple structure
Quasi traveling wave sidecouple structure
Design of a quasi traveling wave side couple RF gun
Quasi traveling wave side couple has stronger focusing and accelerated gradient than DAW.

## Slide 8
Emittance: 5.5 mm-mrad @ 5 nC
This RF gun can generate 10 nC beam
Quasi traveling wave side couple RF gun
This RF gun has total of seven acceleration cavities. These are divided into two standing wave structure of 3 and 4 side coupled cavities respectively.
Maximum E-field at surface: 100 MV/m
Maximum E-field at surface: 120 MV/m
Cathode cell
To avoid beam defocusing, emittance growth and field concentration, a lot of parameters were searched for design.
cathode
Notes: RF gun designed with quasi-traveling wave cavity.
This is whole cavity design.
This RF gun has total of seven acceleration cavities. These are divided into two standing wave structure of 3 and 4 side coupled cavities respectively.
In the cathode cell, We need strong focus field. But it may cause emittance growth. Additionally, we must avoid the E-field concentration.
Designing is very complicated, I automatized this procedure by using downhill simplex method.
Finally we got a very good cavity design.
Result of beam tracking simulation, emittance is 5.5 mm-mrad at 5nC.
In addition, it can generate 10 nC beam. It is enough margin.

## Slide 9
Beam tracking simulation result
Emittance 5.5 mm-mrad
Size 0.4 mm
Energy spread 0.6%
Bunch shape
Gun Exit
5 nC
10 nC
Notes: This is the result of beam tracking simulation.
Emittance is very good and beam size will be small. It will be almost parallel beam at gun exit.
And energy spread is very small.

## Slide 10
RF-Gun comparison
DAW-type RF gun (90 MV/m, 5 mm-mrad, 3.2 MeV)
BNL-type RF gun (120 MV/m, 11.0 mm-mrad, 5.5 MeV)
Quasi traveling wave side couple RF gun (100 MV/m, 6mm-mrad, 13.5 MeV)
BNL (3.8 mm)
QTW (0.2 mm)
DAW (1.7 mm)
Beam Size
Notes: で実際にどの程度，ビームが改善されているかをDAW型や一般的なRF gunにつかわれるBNL型と比較してみました．

## Slide 11
coupling cavities
accelerating cavity
cathode
Cavity design
beam
90 deg hybrid
RF
Field calculation
No reflection to klystron
Notes: This is whole cavity shape. It is little bit complicated shape.
RF fed by using 90deg hybrid in to two ports.

## Slide 12
Mechanical design and manufacturing
Notes: We finished cavity fabrication.
brazing

## Slide 13
A-1 RF gun
- Quasi-travelling wave side couple RF-Gun
Yb based laser system
Existing DC-Gun & pre-buncher
Installed RF-Gun
Chicane for bunch compression
30ps => 10ps

## Slide 14
Installed RF gun
RF
Cathode
beam
Laser port
90 deg Hybrid
- 10 MeV @ 20 MW is designed value
- 6 MeV @ 12 MW is maximum power => Phase slip , Large energy spread

## Slide 15: IrCe cathode

## Slide 16: Cathode : Advantage of metal composite cathode (LaB6 or Ir5Ce )
Justin Jimenez, A Systematic Cathode Study , Ph.D Thesis, Monterery, California
Physica Scripta. Vol. T71, 39-45, 1997.
Cathodes for Electron Guns
G. I. Kuznetsov
Low Workfunction (2.8 eV) and enough QE (10-4) at room temperature.
Inactive in air
Recover by heating or laser cleaning
Best choice
for SuperKEKB 5 nC long time operation

## Slide 17
10-4
10-5
Chart: Lifetime (hour)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48
IrCe | 4.5973e-05 | 5.031e-05 | 5.1572e-05 | 5.1493e-05 | 4.7787e-05 | 5.1414e-05 | 4.8023e-05 | 4.7629e-05 | 4.621e-05 | 4.0615e-05 | 4.0925e-05 | 3.911e-05 | 3.8605e-05 | 3.9795e-05 | 3.7437e-05 | 3.6742e-05 | 4.3358e-05 | 4.4764e-05 | 4.403e-05 | 3.9224e-05 | 4.2479e-05 | 4.096e-05 | 4.296e-05 | 4.4332e-05 | 4.2747e-05 | 4.1657e-05 | 4.776e-05 | 4.1744e-05 | 4.0356e-05 | 3.9094e-05 | 3.7247e-05
LaB6 | 4.086e-05 | 3.555e-05 | 3.6631e-05 | 3.2256e-05 | 3.2046e-05 | 2.9486e-05 | 2.7039e-05 | 2.8325e-05 | 2.4266e-05 | 2.2942e-05 | 2.183e-05 | 2.0947e-05 | 1.9323e-05 | 1.8752e-05 | 1.7533e-05 | 1.7465e-05 | 1.5575e-05 | 1.4985e-05 | 1.5869e-05
Lifetime measurement（LaB6 / Ir5Ce）
Continuous pulse laser 200μJ@266nm)
Irradation => 2.5 nC emission
Condition

## Slide 18: Ir5Ce Cathode
Chart: Energy density of cleaning laser(μJ/mm2)
| 0 | 100 | 200 | 350 | 450 | 650 | 1000
LaB6@266nm | 2.551e-06 | 1.212e-05 | 2.191e-05 | 8.25e-05 | 5.314e-05 | 5.314e-05 | 6.273e-05
LaB6@532nm | 2.2662e-06 | 2.115e-05 | 2.6172e-05 | 9.6194e-05 | 0.00017493 | 3.8669e-05
Ir5Ce@266nm | 3.507e-06 | 2.215e-05 | 5.51e-05 | 8.61e-05 | 0.0001019
Quantum efficiency improvement by Laser cleaning
[SUPER-KEKB e Linac]
Laser Power ; 233μJ/pulse
（λ=266nm）
Target value ; 5nC
HV = 16kV
Vacuum ; 5.8×10-6 Pa
Cleaning time ; 10 min
Condition
×２０
Max QE = 1.00×10-4
Laser cleaning
×20
Lower energy density is enough to activate Ir5Ce
QE = 5.00×10-6
Non activation
LaB6
Carbon
Oxigen
SEM-EDX
Ir5Ce
Carbon
SEM-EDX
No oxidization is observed

## Slide 19: Laser system for A-1 RF-Gun

## Slide 20: Requirement of laser system for RF-Gun
Laser energy
  500 mJ UV for Ir5Ce cathode
  50 mJ UV for Ce2Te cathode
50 Hz, 2-bunch (96ns spacing) => Difficult to adopt commertial products using regenerative amplifier. => Multi-pass amplifier or Special regenerative amplifier
Temporal pulse shaping
  Reduction of energy spread due to longitudinal wakefield
  Rhombus shape for laser injection with angle (higher QE) => Broadband laser crystal (Yb or Ti:Sapphire)
Continuous operation (limited cost / human resource)
  Support cost for commertial product is very high. (10-20万円=1,000-2,000$/day/person + a (margin) )
  No laser system company in Japan.
  Recovering time.

## Slide 21: Required laser pulse energy
5nC
Ce2Te
ATF
Offline measurement
P-polarization
Offline measurement
S-polarization
Normal injection (old 3-2)
Inclined injection
Charge( C )
Laser power ( J )
QE=10-3
QE=10-4
QE=10-5
Current laser energy(500μJ)

## Slide 22: How to generate 2-bunch
Amplification time of standard regenerative amplifier (usually adopted in commertial product) is around 1 ms.
Two regenerative amplifier (not good)
Large regenerative amplifier (built & failed)
  Unstable output energy due to low gain.
  Difficult to compensate thermal lens.
High gain fast regenerative amplifier (built & failed)
  Difficult to reduce the ghost pulse from first bunch due to limted extinction ratio of pockels cell.
Multi-pass amplifier (current configuration)
  More gain is required for the balanced 2-bunch.
OPCPA (future candidate)

## Slide 23
Pulse shaping is necessary at angled injection for higher QE.
One of problem is beam hole in the cavity is too small. (less than cathode diameter.)
Redesign is required.
Beam
Mirror in vacuum
Rhombus pulse shaping for angled injection

## Slide 24: Energy spread reduction by pulse shaping
Gaussian
Square
5nC
10nC
15nC
20nC
20nC
15nC
10nC
5nC
5nC electron
15nC
Primary beam for positron production
t
t
Energy spread of 0.1% is required for SuperKEKB synchrotron injection.

## Slide 25: Properties of laser medium
LD Pump
(808nm)
Nd:YVO4
Nd:YAG
SHG(532nm) 40%
FHG(266nm) 20%
5HG(213nm) 3%
τ～200μs, 40%
Nd-doped
Yb-doped
Ti-doped
LD Pump
(941/976nm)
Yb-glass
Yb:YAG
Yb:BOYS
1064nm
808nm
941/976nm
1040nm
τ～900μs, 40%
Pump
(808nm)
Nd:YAG
SHG
40%
1064nm
808nm
Ti:Sapphire
532nm
800nm
τ～3μs, 40%
τ=200μs, 40%
○ 4-state laser is easy to operate.
○ High power pump LD is available.
○ Large crystal is available
× Pulse width is determined by SESAM. (Gaussian)
○ Wide bandwidth => pulse shaping
○ Long fluorescent time => High power
○ Fiber laser => Stable
○ Small state difference
× ASE
× Absorption
○ Very wide bandwidth
○ High breakdown threshold
× Low cross section
× Short fluorescent time => Q-switched laser is required for pumping
Pump
TW laser is based on Ti-Sapphire
SHG(520nm) 40%
FHG(260nm) 20%
5HG(208nm) 3%
SHG(400nm) 40%
THG(266nm) 20%
FHG(200nm) 10%
Best for RF-Gun
Nd laser system for 3-2 RF-Gun
Ti:Sapphire laser system for beam monitor.

## Slide 26: Yb laser system (Present status)
Yb Fiber Laser
frep=52MHz→10MHz
Amplitude modulator x 2
Fiber strecher
& wavelength selection
Yb:YAG
5-pass Amplifier ×4stage
Pulse
Compression
Yb:YAG
Regenerative
Amplifier
Yb Fiber Amplifier
Yb Fiber
Oscillator
Yb Fiber
Amplifier x 2
(20W + 70W pump)
λ0→1030 - 1040nm
Yb:YAG laser
frep=52MHz
Yb PCF Amplifier
(70W pump)
Pulse picker
frep=10 MHz→50 Hz
Wavelength
conversion
0.7 mJ @ 258nm
7 mJ @ 1030nm
Yb:YAG
Multipass
Amplifier
ASE problem
Failed
Yb:YAG
5-pass Amplifier

## Slide 27
Yb Fiber Oscillator
Yb Fiber
←
←
WDM
LD
Transmission
grating pair
Yb fiber oscillator:
30 fs is possible using non-linear polarization rotation.
52 MHz is not suitable => 114 MHz will be installed
Improved items in FY2013:
Transmission grating => Stable modelock (higher efficiency)
Super-invar breadboard => Improve thermal stability.
Piezo mirror on large lead block => Reduce vibration.
Broadband oscillator (No.2) is stable.
Remaining problem:
LD was sometimes broken.
Bunch structure at higher output power. => SESAM is not effective. => Replace some components.
1030nm oscillator is not stable
1030nm component of broadband oscillator is small => large ASE

## Slide 28
Yb:YAG fiber oscillator
Two 52 MHz oscillators are installed for the underground laser room.
Second oscillator is very stable
Phase stability (sigma)
Oscillator1 : 2.38 deg
Oscillator2 : 0.58 deg = 560 fs
Oscillator1: Narrow (Less ASE)
Oscillator2: Broadband (Stable)
Yb:YAG bandwidth

## Slide 29: Pulse shaping using strecher
30 ps
Measured by streak camera
1740-grooves/mm
Telescope lens
Rectangular-like 30 ps pulse width was obtained.
Strecher

## Slide 30: Yb:YAG solid state amplifier
Improvement of heat conductivity by Au-Sn vacuum soldering.
Copper plate
Au-Sn coating
5 Hz => 25 Hz operation was achieved.

## Slide 31
1pass
LD
Laser Diode
2pass
3pass
4pass
5pass
Original multi-pass amplifier (5-pass)
Balanced offset lens to avoid damage.
To obtain higher gain,
=> Higher pumping density
Thermal lens
Focused type amplifier to avoid thermal lens.

## Slide 32
New high gain multi-pass amplifier(10-15 pass x 2 loop)
to simplify the laser
LD
Laser Diode
INPUT
OUTPUT
1pass
10-15pass
←

## Slide 33: Issues on Yb based laser system
Yb-fiber oscillator
  1030nm oscillator is not stable.
  Broadband oscillator is very stable => Further ASE reduction is required.
Yb-fiber amplifier
  Lack of pulse energy =>
  Lifetime and stability of PCF fiber => Improve the injection
Yb-disk amplifier: (Regenerative amplifiers were failed) => Multi-pass amplifier for 2-bunch operation. => More gain is required for balanced 2-bunch energy.
  5 Hz => Soldered cryatal => 25 Hz operation => x 2 system => 50Hz before May 2015
  Reduce thermal lens effect and simplify laser system => Focused type high gain multipass amplifier x2 + Non-focused multipass amplifier
Stability improvement
  Casing of each block.
  Gas filled or vacuum laser transportation to improve pointing stability.
  Assemble on one large optical table (new laser room).
  Feedback (pointing / amplitude).
  Increase monitor points (pointing / power / beam pattern).

## Slide 34: Comissioning of A-1 RF-Gun

## Slide 35: RF voltage
 | RF power [MW] | Maximum surface E-field [MV/m]
DAW @ 3-2 | 3.5 | 150
QTW @ A-1 target | 20 | 120
QTW achieved @ A-1 | 14 | 85
One week RF ageing reach this target.
cathode
Beam hits anode.
Anode shape should be changed. (large beam hole)
DAW type RF gun is effective shape for multipactoring?

## Slide 36
A-1 RF gun results
5.6 nC was achieved.
However beam profile is not good.
3 nC beam delivery was achieved.

## Slide 37: Charge history of A-1 RF-Gun (3nC)
QE : 3nC = 14nJ / 300μJ = 4.5×10-5 (QE)

## Slide 38
Emittance measurement
Q scan method using screen
monitor
Normalized emittance
X : 13.4 +/- 5.9 [mm-mrad]
Y : 8.05 +/- 0.47 [mm-mrad]
beam charge : 0.6nC
beam energy : 30 MeV
Normalized emittance
X: 95.0 ±27.4 mm-mrad
Y: 42.0 ±31.1 mm-mrad
(including the beam position jitter.)
Wire scanner
at B sector

## Slide 39
Bunch compression and streak camera
Compression at chicane
10 psec
No compression
20 psec

## Slide 40: Summary of issues
RF-Gun cavity
  Disk and washer (DAW) : very fast RF ageing, 2 MeV is not enough.
  Quasi travelling wave side couple structure :
    Lower electric field than designed value. => Thermal electron gun will recover for positron generation in May 2015.
Cathode
  Room temperature Ir5Ce cathode seems best cathode !
  Laser injection angle for surface plasmon is effective.
  R&D for the QE improvement and cleaning.
  Preparation to use alkaline cathode
Laser & control
  Nd based laser system : 3-2 RF-Gun
    Oscillator: RF synchronization precision is not enough.
    Repetition rate 10 Hz operation => how to upgrade to 50 Hz ?
  Yb based laser system : A-1 RF-Gun => next page
Beam transportation and diagnostics
  Beam loss in first accelerating structure (will be solved in May 2015.)
  Old streak camera for beam diagnostics. (renewed for laser diagnostics)
  Single cavity RF-Deflector installation.

## Slide 41: Plans & Schedule following LINAC group strategy and RF-Gun review (last week)

## Slide 42: Schedule
These few months:
  Reconfigure thermal gun for positron generation
  Step by step RF-Gun RF ageing.
  New laser system in ground laser room.
    Increase pulse energy from fiber laser
    Simplify the laser system (new multi-pass amplifier)
Next summer:
  Second RF-Gun (nomal laser injection / cavity modification / cathode change)
  Simple Nd amplifier for Phase-I & II stable injection
10 ps gaussian is enough for Phase-I (1nC) & II (2nC), postponed the pulse shaping until Phase-III
Following the RF-Gun reviewer’s comments
(Postponed the pulse shaping until Phase-III )

## Slide 43: Strategy for emittance preservation and energy spread
Emittance preservation
  Alignment : Initial alignment / Continuous monitor / Active mover / Beam based alignment 0.3 mm mis-alignment tolerance for 2 nC (until Phase-II) 0.1 mm mis-alignment tolerance for 5 nC (Phase-III) => shorter bunch (5 ps) is required for 0.3mm mis-alignment
  Offset injection compensate the transverse wakefield (RF Deflector will be installed for beam diagnostics for offset injection)
Energy spread
  0.1 % is required for SuperKEB injection
  10 ps gaussian pulse is enough for 2 nC (until Phase-II)
  Laser pulse shaping is only required for Phase-III
  Bunch compression to 5 ps is required for Phase-III depending on the mis-alignment.

## Slide 44
Thermionic DC gun
RF gun
SHB1
SHB2
prebuncher
buncher
Acc.tube
Acc.tube
Energy slope
30 MeV
20 psec
Chicane
Bunch compression
20 psec
triplet
5 nC
Low emittance
10 nC
for positron primary
Beam line will be upgrade on up and down.
Thermionic DC gun will be installed to upper beam line.
70 MeV

## Slide 45: Reconfiguration of A-1 injector area
KL_A1_A
KL_A1_B
RF-Gun1
RF-Gun2
加速管

## Slide 46
Second RF gun on the 45 degree line
Studies on
Improved RF-Gun cavity
Normal laser injection
Cathode change including alkaline cathode
Normal laser injection
Angled laser injection

## Slide 47
Second Side coupled Quasi-travelling wave RF-Gun
Conditioning progress was too slow. Frequently brake down is big problem.
Cathode rod contact?
Cathode material fixation?
Cathode material sputtering due to laser?
We have to separate causes of brake down.
Cavity conditioning, used dummy cathode rod with out cathode material (all Cu).
Replace new cathode rod with material (new fixation is shrinkage fit).
For reduce multipactoring effect, another cathode cell design is required.
Second RF-Gun under brazing
shrinkage fit
Current cathode
New cathode

## Slide 48: Simplify and stabilize our laser system without pulse shaping
Yb-doped fiber oscillator with Transmission grating
PCF Yb-doped fiber amplifier
Pulse picker
Commertial Nd:YAG rod
multipass amplifier (10 Hz => 50 Hz)
Yb:YAG thin-disk multipass amplifier
(25 Hz x 2)
114.2 MHz
@ 1030 nm
@ 1064 nm
LIEKKI Yb-doped fiber amplifier
Pulse picker
Grating pair
Fiber Amplifier @1030 nm
Fiber Amplifier @1064 nm
Spatially dispersed
Yb fiber Oscillator
Menlo
Optilab YDFA-r-40-S, Output power of 20W
\3,500,000
Existing laser system
Simple Nd amplifier laser system without pulse shaping according to RF-Gun reviewer’s comment

## Slide 49: Strecher for Yb:YAG & Nd:YAG
2.0nm
 | Yb:YAG | Nd:YAG
Center wavelength | 1030 nm | 1064 nm
Gain spectrum width | ~2 ns | ~0.5ns
Distance of the Stretcher to 30 ps | 1.5 m | 6 m (×4)
Grating pair
30 ps
Gain spectrum of Yb:YAG
Distance of grating pair

## Slide 50: Improvement of fiber collimation
Fiber coupler
Cooling system
Fiber coupler in ERL
Drum Lens
PCF fiber damage is one issue => Improve the fiber collimation
Higher output pulse energy from fiber amplifier
=> Reduce number of stages of Yb:YAG multi-pass amplifier

## Slide 51: Temperature dependence of Yb:YAG
Improvement of thermal and emission property (Thermal lens effect) (Excitation density)
300K
30kW/cm2
Pertier
GM+He
300K P/P0 = exp(g0z) ～2 150K → g = 7 [cm-1]
10 W/m/K , dn/dT = 8ppm/K @ 300K
25 W/m/K , dn/dT = 3ppm/K @ 150K
↑150K 1/6 Thermal lens
Same gain @ 1/3 excitation density →
↓
150K => 1/20 thermal lens

## Slide 52: Schedule
These few months:
  Reconfigure thermal gun for positron generation
  Step by step RF-Gun RF ageing.
  New laser system in ground laser room.
    Increase pulse energy from fiber laser
    Simplify the laser system (new multi-pass amplifier)
Next summer:
  Second RF-Gun (nomal laser injection / cavity modification / cathode change)
  Simple Nd amplifier for Phase-I & II stable injection
10 ps gaussian is enough for Phase-I (1nC) & II (2nC), postponed the pulse shaping until Phase-III
Following the RF-Gun reviewer’s comments
(Postponed the pulse shaping until Phase-III )